# Concrete Strength Verification Report & Strategy

Project: Residential Building (Basement, G+1)
Location: Kribi, South Region, Cameroon
Concrete Grade: C25/30 (Target 30.0 MPa at 28 Days)
Date of Generation: September 17, 2026

--------------------------------------------------------------------------------

# Executive Summary: Mandatory vs. Supplementary Testing

Question: Must all these tests be done for one building, or will only one test do?
Answer: No single test can replace the others. A minimum of TWO tests are legally mandatory for every structural pour: 1) Fresh Concrete Testing (to authorize the pour) and 2) 28-Day Laboratory Cube Crushing (to legally certify the strength). The Non-Destructive and Core Extraction tests are supplementary—they are only deployed if the mandatory laboratory cubes fail, are lost, or if on-site curing quality is heavily doubted.

# 1. Fresh Concrete Testing (On-Site)

When exactly to execute: Immediately upon arrival on-site (ready-mix) or right after batching on-site, strictly BEFORE the concrete is poured into the formworks.
Importance: Ensures the mix is workable, has the correct water-to-cement ratio, and isn't too hot (critical in Kribi's climate to prevent flash setting).
Why it cannot be replaced: You cannot wait 28 days for a lab result to find out a mix was too wet. This is the only gatekeeper preventing bad concrete from entering the structure.
What to do if it fails: REJECT THE BATCH immediately. Do not pour it. Instruct the supplier to provide a new batch with the correct water/cement proportions.

| Test Parameter | Target | Measured Field Value | Status |
| --- | --- | --- | --- |
| Slump Test | 75 mm – 100 mm | 85 mm | Pass |
| Temperature | ≤ 32.0°C | 28.5°C | Pass |
| Air Content | 1.5% – 3.0% | 2.1% | Pass |

# 2. Laboratory Compressive Strength (150mm Cube Crushing)

When exactly to execute: Samples are cast during the physical pour on-site. The crushing is executed precisely at 7 days, 14 days, and 28 days after the pour.
Importance: This is the legal gold standard and primary verification that the mix design is capable of reaching the structural engineer's required 30.0 MPa capacity.
Why it cannot be replaced: It is the only direct, controlled measurement of the concrete mix's true compressive strength potential. Field testing only measures surface hardness, not deep capacity.
What to do if it fails: If the 7-day test fails, HALT construction above that element. If the 28-day test fails, immediately order Non-Destructive Testing (Section 3) on the actual building to check if the issue was just a bad lab sample or a true structural failure.

| Test Interval | Required Minimum | Measured Average | Status |
| --- | --- | --- | --- |
| 7-Day (Batch A) | 19.5 MPa (~65%) | 21.2 MPa | Pass |
| 14-Day (Batch B) | 27.0 MPa (~90%) | 28.1 MPa | Pass |
| 28-Day (Batch C) | 30.0 MPa (100%) | 32.4 MPa | Pass |

# 3. Non-Destructive Testing (In-Situ Rebound Hammer)

When exactly to execute: After the concrete has fully hardened (typically at or after the 28-day mark), or whenever lab cubes fail or are missing.
Importance: Verifies that the actual poured concrete in the field matches the lab results. Lab cubes are cured perfectly in water; this tests if the on-site curing was done properly.
Why it cannot be replaced: Unlike lab cubes, this tests the structure itself. Unlike core extraction, it does not damage or drill holes into your finished columns.
What to do if it fails: If Rebound Hammer tests indicate strength significantly below 30 MPa, you must escalate to Core Extraction Testing (Section 4) for a definitive answer.

| Structural Element | Target Strength | Measured Field Strength | Status |
| --- | --- | --- | --- |
| Retaining Walls | 30.0 MPa | 33.1 MPa | Pass |
| Ground Columns | 30.0 MPa | 31.8 MPa | Pass |
| Ground Beams | 30.0 MPa | 34.2 MPa | Pass |

# 4. Core Extraction Testing (Destructive / Last Resort)

When exactly to execute: Only deployed as an absolute last resort if both 28-day Lab Cubes and Non-Destructive tests show failing grades, or during forensic audits.
Importance: Provides the undeniable, actual physical compressive strength of the structural element exactly as built.
Why it cannot be replaced: It is the absolute final say in a dispute. Rebound hammers estimate strength; cores physically measure the actual structure's strength.
What to do if it fails: If the core crushes below the required safety margins, the structural element MUST be demolished and rebuilt, or heavily retrofitted (e.g., carbon fiber wrapping, steel jacketing) by structural specialists.

# 5. Verification Sign-Off

By signing below, the verifying engineer confirms tests were conducted per Eurocode 2 (EN 1992).

Name of Verifying Engineer: _______________________________________
Professional License Number (ONIGC/Equivalent): _____________________
Engineering Firm / Control Bureau: __________________________________
Date of Verification: ______________________________________________